# SECTION 602 – CONCRETE DRIVEWAYS

602-1  DESCRIPTION

This work shall consist of the construction of new, removed, and replacement of air-entrained portland cement 6-inch or 8-inch concrete in accordance with these specifications and standard details at the locations and to the lines and grades shown on the plans or as directed by the ENGINEER.

602-2  MATERIALS

Materials for portland cement concrete shall meet the requirements of Subsection 501-2.

602-3  CONSTRUCTION REQUIREMENTS

Construction requirements shall conform to Subsection 501-3 with the following additional provisions:

602-3.1  CONTRACTOR'S STAMP OR NAME PLATE.  The CONTRACTOR shall mark in each driveway, either by stamping or by inlaying, an approved metal plate conforming to Subsection 501-3.15.

602-3.2  BACKFILL.  The 6-inch or 8-inch concrete shall be backfilled within 14 days of placement to a level width of at least 2 feet along all edges and to a height equal to the top finished grade of the driveway.  The backfill shall be compacted in accordance with Section 202 "Excavation and Embankment."

602-3.3  SIX-INCH CONCRETE REMOVAL.  Six-Inch Concrete Removal shall consist of removal of concrete that is 5 inches or greater in thickness and less than 8 inches.  .  Disposal shall be in accordance with Subsection 501-3.16.

602-3.4  SEALING JOINT.  Joints sealed shall be sealed in accordance with Subsections 501-3.22 and 501-2.9 and shall be incidental to other bid items.

602-3.5  TREE REMOVAL OR TREE ROOT CUTTING.  Construction methods and measure and payment shall meet the requirements of Section 201.

602-3.6  FORMS.  Forms shall conform to Subsection 501-3.11.  All driveway forms for 6-inch or 8-inch concrete shall be set at a 90-degree angle to the street or curb and gutter alignment unless otherwise approved by the ENGINEER.

602-3.7  JOINTS.  Expansion joint materials shall not be used in 6-inch or 8-inch concrete aprons unless approved by the ENGINEER.  Jointing shall conform to Detail Drawings 600-7 and 600-8 or joints approved by the ENGINEER.  Jointing shall be done with appropriate jointing tools or sawed.  All joints sawed into driveways must be sawed with a double blade in order for joint sealant to be installed to proper width and depth.

602-3.8  CONCRETE QUALITY CONTROL AND SUBGRADE TESTING.  Testing shall conform to Section 501-3.4.  Payment shall be considered incidental to other bid items.

602-4  MEASUREMENT AND PAYMENT

602-4.1  6-INCH CONCRETE.  Six-Inch Concrete shall be measured by the square foot (SF) and paid for at the unit price bid for "6-Inch Concrete " complete, in place, and accepted by the ENGINEER.

602-4.2  8-INCH CONCRETE.  Eight-Inch Concrete shall be measured by the square foot (SF) and paid for at the unit price bid for "Eight-Inch Concrete " complete, in place, and accepted by the ENGINEER.

602-4.2A  8-INCH CONCRETE REMOVAL.  Eight-inch or thicker concrete removed and disposed of shall be measured by the square foot (SF) and paid for at the unit price bid for "Eight-Inch Concrete Removal."  All 8-inch or thicker concrete removed shall be disposed of in accordance with Subsection 501-3.16.

602-4.3  SIX-INCH CONCRETE REMOVAL.  Six-Inch Concrete removed and disposed of shall be measured by the square foot (SF) and paid for at the unit price bid for "Six-Inch Concrete Removal."  All 6-inch concrete removed which is less than 8 inches in thickness will be paid for under this item.