## SECTION 405 – CRACK TREATMENTS

405-1  DESCRIPTION

This work shall consist of applying a crack sealant material into or above existing cracks to prevent the intrusion of water and incompressible material into the cracks and to reinforce the adjacent pavement.  There are two methods of crack treatments: crack sealing and crack filling.  The ENGINEER shall determine which cracks are candidates for which method of crack treatment.

  - METHODS

405-2.1  Crack Sealing.  This method of crack treatment shall be utilized when the crack shows significant signs of vertical or horizontal movement, or where crack edges may exhibit edge deterioration or displacement.

405-2.2  CRACK FILLING.  This method of crack treatment shall be utilized when the crack shows very little sign of vertical or horizontal movement.

405-3  MATERIALS

The types of materials essentially comprise three material groups according to their composition and manufacturing process.  The principal material groups and types are as follows:

1.  Cold-applied thermoplastic bituminous materials.

a.  Liquid asphalt (emulsion).

b.  Polymer-modified liquid asphalt.

2.  Hot-applied thermoplastic bituminous materials.

- Asphalt cement.

- Fiberized asphalt.

- Rubberized asphalt.

- Low-modulus rubberized asphalt.

3.  Chemically cured thermosetting materials.

- Self-leveling silicone.

Asphalt cutbacks, mineral-filled asphalts, and sand-asphalt mixtures will not be accepted.

The following table shows the material types that possess most of the above properties. It also shows the recommended application methods and requirements for each type of material used.

| Material Type | Applicable Specifications | Recommended Application |
| --- | --- | --- |
| Asphalt Emulsion | ASTMb D977, AASHTOc M140, ASTM D2397, AASHTO M208 | Filling |
| Asphalt Cement | ASTM D3381, AASHTO M20, AASHTO M226 | Filling |
| Fiberized Asphalt | Manufacturer’s recommended specs | Filling |
| Polymer-Modified Emulsion | ASTM D977, AASHTO M140, ASTM D2397, AASHTO M208 | Filling |
| Asphalt Rubber | State specs, ASTM D5078 | Sealing |
| Rubberized Asphalt | ASTM D1190, AASHTO M173, Fed SS-S-164 | Sealing |
| Low-Modulus Rubberized Asphalt | State-modified ASTM D3405 specs | Sealing |
| Self-Leveling Silicone | ASTM D5893 | Sealing |

A.  Emulsion and Asphalt Cement Sealants.  This material shall be placed flush in an unrouted, non-working crack.

B.  Rubberized Asphalt Sealants.  This material shall be placed flush or overbanded in routed, working cracks.

C.  Self-Leveling Silicone Sealants.  This material shall be placed recessed in routed, working cracks.

D.  Fiberized Asphalt Sealants.  This material shall be placed overbanded in unrouted, working cracks.

405-4  PLACEMENT CONFIGURATION

Sealant and filler materials can be placed in numerous configurations.  These placement configurations are grouped into six categories.

1.  Flush Fill.  This configuration places the material into the existing unrouted crack and the excess material is struck off.  Standard Detail 400-2 (A) illustrates the flush fill method.

2.  Reservoir.  This configuration places the material only within the confines of the routed crack.  The material placed is either flush with or slightly below the pavement surface.  Standard Details 400-2 (C) and (E) illustrate the reservoir-type method.

3.  Overband.  This configuration places the material into and over an unrouted crack.  The excess material shall then be squeegeed to straddle the crack to a minimum width of 1½ inches on either side.  Standard Detail 400-2 (B) illustrates the overband method.

4.  Combination (Reservoir and Overband).  This configuration places the material into and over a routed crack.  The excess material shall then be squeegeed to straddle the crack to a minimum width of 1½ inches on either side.  Standard Details 400-2 (D) and (F) illustrate the combination method.

5.  Bond Breaker Material.  If the crack continues below the routed crack, a bond breaker material, nonabsorbent closed cell, such as polyethylene foam backer rod, shall be placed at the reservoir bottom of a working crack prior to the sealant application.  The backer rod prevents the sealant material from running down into the crack during application.  The backer rod material must be a minimum of 25 percent wider than the width of the crack reservoir for it to maintain its vertical position and to provide shape for the material.  Standard Details 400-2 (E) and (F) illustrate the placement of the backer rod material.

6.  Routed/Sawn Cracks.  Working cracks that are relatively straight and are accompanied by edge deterioration are candidates for crack cutting.  Crack cutting shall be performed in such a manner so as not to create any additional damage to the existing pavement.  High-production machines that follow cracks well and produce minimal spalls or fractures shall be equipped with controls for varying the depth of the cut and the width settings.  Standard Details

400-2 (C) through (F) illustrate crack cutting dimensions.

405-5  MATERIAL REQUIREMENTS

The crack sealant compound shall be packaged in sealed containers.  Each container shall be clearly marked with the name of the manufacturer, the trade name of the sealant, the type of sealant, the weight, the manufacturer's batch and lot number, the pouring temperature, and the safe heating temperature.

Prior approval of any specific sealant material shall be required before it can be used on the project.

A copy of the manufacturer's recommendations pertaining to the heating and application of the joint sealant material shall be submitted to the ENGINEER before the commencement of work.  These recommendations shall be adhered to and followed by the CONTRACTOR.  The temperature of the sealer in the field application equipment

shall not exceed the safe heating temperature recommended by the manufacturer.  Any given quantity of material shall not be heated at the pouring temperature for more than six (6) hours and shall never be reheated.  Material shall not be placed if the temperature is below the manufacturer's recommended minimum application temperature.

Mixing of different manufacturer's brands or different types of sealant shall be prohibited.

Sealant materials may be placed during a period of rising temperature after the air temperature in the shade and away from artificial heat has reached 40F and indications are for a continued rise in temperature.  During a period of falling temperature, the placement of sealant material shall be suspended when the air temperature in the shade and away from artificial heat reaches 40F.  Sealants shall not be placed when the weather or roadbed conditions are unfavorable.

405-6  CRACK TREATMENT PROCEDURES AND EQUIPMENT

The following table shows the required crack treatment equipment characteristics and recommendations.

| Operation | Type of Equipment | Recommendations |
| --- | --- | --- |
| Crack Cutting (if required) | Vertical-Spindle Router | Use only with sharp carbide-tipped or diamond router bits |
|  | Rotary-Impact Router | Use only with sharp carbide-tipped router bits |
|  | Random Crack Saw | Use only on fairly straight cracks Diamond blade saw, 200-mm maximum diameter |
| Crack Cleaning/ Drying | Blowers (Backpack & Power- Driven) | Not recommended - Insufficient blast velocity (60 to 100 m/s) |
|  | Air Compressor | Equipped with oil and moisture filters Pressure - 690 kPa minimum Flow - 0.07 m3/s minimum Velocity - 990 m/s minimum |
|  | Hot-Air Lance | Velocity - 610 m/s minimum Temperature - 1370C minimum No direct flame on pavement Highly Recommended Velocity - 915 m/s minimum Temperature - 1650C minimum |
|  | Sandblaster | Acceptable air compressor (minimum 690 kPa pressure and 0.07 m3/s flow) Minimum 25-mm-inside-diameter lines and 6-mm-diameter nozzle |
|  | Wirebrush | Do not use with worn brushes Not recommended for cleaning previously-treated cracks as there is a tendency to smear material |
| Material Installation | Pour Pots | Not recommended for production operations |
|  | Asphalt Distributor | Not suitable for fiber- or rubber-modified asphalt materials |
|  | Melter-Applicator | Direct-heat kettles not suitable for fiber- or rubber-modified asphalt materials Indirect-heat kettles should be equipped with: * Double-boiler, mechanical agitator with separate automatic temperature controls for oil and melting chamber * Sealant heating range to 230C * Full-sweep agitator * Accurately calibrated material and heating oil temperature gauges |
|  | Backer Rod Installation Tools | Maintains proper recess Does not damage backer rod |
|  | Silicone Pump & Applicator | Flow Rate - 0.25 L/s minimum Hose line with Teflon; all seals and packing made from Teflon |
| Material Finishing | Squeegee | Heavy-duty, industrial U- or V-shaped |
| Blotting (if required) | Paper Wand | To prevent tracking |

If tracking of the sealant is present, blotting or tissuing will be required.  Blotting may consist of sand limestone dust or crusher dust placed directly on top of the treatment material.

405-7  TRAFFIC CONTROL PLAN AND QUALITY OF DEVICES

The CONTRACTOR shall be responsible for all traffic control devices needed for the completion of the crack treatment operation.

Traffic Control Devices used on the project will be rated according to the American Traffic Safety Services Association's (ATSSA) Quality Standards for Work Zone Traffic Control Devices.  The definitions of "acceptable," "marginal," and "unacceptable," and the evaluation guidelines shall be defined in ATSSA's Quality Standards for Work Zone Traffic Control Devices.

All traffic control devices shall be retroreflective.

An approved traffic control plan shall be submitted three days prior to its use.

Traffic control plan and devices shall be considered incidental to other bid items.

The CONTRACTOR shall broom off the excess debris and remove the traffic control devices after the crack treatment operations are completed.

405-8  MEASUREMENT AND PAYMENT

405-8.1  EMULSION AND ASPHALT CEMENT SEALANTS.  The Emulsion and Asphalt Cement Sealants shall be measured by the linear foot (LF) and paid for at the unit price bid for "Emulsion and Asphalt Cement Sealants" complete, in place, and accepted by the ENGINEER.

405-8.2  RUBBERIZED ASPHALT SEALANTS.  The Rubberized Asphalt Sealants shall be measured by the linear foot (LF) and paid for at the unit price bid for "Rubberized Asphalt Sealants" complete, in place, and accepted by the ENGINEER.

405-8.3  SELF-LEVELING SILICONE SEALANTS.  The Self-Leveling Silicone Sealants shall be measured by the linear foot (LF) and paid for at the unit price bid for "Self-Leveling Silicone Sealants" complete, in place, and accepted by the ENGINEER.

405-8.4  FIBERIZED ASPHALT SEALANTS.  The Fiberized Asphalt Sealants shall be measured by the linear foot (LF) and paid for at the unit price bid for "Fiberized Asphalt Sealants" complete, in place, and accepted by the ENGINEER.

405-8.5  BOND BREAKER MATERIAL.  Bond Breaker Material shall be measured by the linear foot (LF) and paid for at the unit price bid for "Bond Breaker Material" complete, in place, and accepted by the ENGINEER.

405-8.6  ROUTED/SAWN CRACKS.  The Routed/Sawn Cracks shall be measured by the linear foot (LF) and paid for at the unit price bid for "Routed/Sawn Cracks" complete, in place, and accepted by the ENGINEER.